## Slide 1
Asha A
Department of Science and Humanities
ENGINEERING CHEMISTRY

## Slide 2
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Class content:
Commercial Polymers
  Butyl Rubber
  Biodegradable polymers
  Epoxy Resin

## Slide 3
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Elastomers
The property of a polymer by which it deforms on applying force and regains original shape on release of force is called elasticity
Elastomers have long, coiled and entangled chains which straighten and orient themselves on stretching ; when stress is removed they go back to coiled form

## Slide 4
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Butyl Rubber
Synthetic rubber with diverse applications
Superior to natural rubber in certain properties
Synthesis :
Low temperature copolymerisation of isobutylene and small amount of isoprene(5-10%) dissolved in CH3Cl
Monomers: Isobutylene and 5-10 % isoprene
Source:https://www.researchgate.net/figure/The-process-of-butyl-rubber-polymerization_fig2_330899891
-95oC
AlCl3
CH3Cl

## Slide 5
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Process:
Isobutylene mixed with isoprene is dissolved in CH3Cl
Anhydrous AlCl3 dissolved in CH3Cl is added and the reaction is carried out at a
low temperature of -95oC
A finely powdered butyl rubber is obtained
Isoprene introduces unsaturation in the polymer chain and helps in
vulcanisation
The product is mixed with antioxidants and dried to prevent degradation

## Slide 6
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Properties:
Exceptional resistance to gas and moisture
(water and steam) permeation
Good chemical inertness
Excellent electrical insulation

## Slide 7
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Applications:
Excellent impermeability to gas makes it very useful in seals for vacuum applications
Gas impermeability coupled with its air retention capabilities makes it popular for use in tyre inner liners and inner tubes
Insulation of high voltage wires and cables
Hydraulic applications where synthetic fluids are used

## Slide 8
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Biodegradable Polymers
Every year we produce millions of tons of garbage which we dispose off in landfills
Waste disposal problems of these traditional plastics which are resistant to microbial degradation causes them to accumulate in the environment which is a serious threat to global ecology
Source:http://www.businessworld.in/article/-79-Of-Total-Plastic-Waste-Stored-In-Landfills-Or-Aquatic-Bodies-/26-07-2017-122920/
Source:https://steemit.com/oceans/@alchemylgc/every-minute-one-garbage-truck-of-plastic-is-dumped-into-our-oceans-this-has-to-stop

## Slide 9
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Source:https://ahlaprsacks.com/faq/

## Slide 10
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Biodegradable polymers: Polymers that can be decomposed by the action of microorganisms into water, carbon dioxide, methane and biomass
Biodegradation is a two step process:
  The first step is fragmentation where the polymer macromolecule is broken down into smaller chains or monomers by hydrolysis or oxidation
  The second step is mineralisation by microorganisms .The products are CO2, CH4, H2O or biomass depending on the structure of the fragmented polymer chains and the environment they are exposed to
Source:https://onlinelibrary.wiley.com/doi/full/10.1002/macp.202000017

## Slide 11
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
The susceptibility of a polymer to undergo degradation depends on :
The structure of the polymer, molecular weight, degree of branching, crystallinity and solubility
  Usually polyesters, polyamides, polyurethanes are found to be biodegradable
The environmental conditions like pH, availability of O2, light, temperature, humidity, microorganism etc.

## Slide 12
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Abbreviation | Name of the polymer
PVOH | Polyvinyl Alcohol
PLA | Polylacetic acid
PHB | Polyhydroxybutyrate
PHBV | Poly(hydroxybutyrate-co-hydroxyvalerate)
PCL | Polycaprolactone
PBST | Poly(butylenesuccinate-co-terepthallate)
PBAT | Poly(butyleneadipate-co-terepthallate)
Examples of Biodegradable polymers
Source:https://www.intechopen.com/books/polymer-science/polymers-and-the-environment

## Slide 13
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Biodegradable polymers
Natural
Synthetic
Collagen
Cellulose
Starch
Chitosan
Fibrin
Polyesters
Polyanhydrides
Polyphosphazenes
Polyphosphoesters

## Slide 14
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Biodegradable plastics are commonly produced from renewable raw materials, micro-organisms, non- renewable raw materials like petrochemicals
Natural biodegradable polymers are derived from renewable resources , e.g., starch, cellulose, proteins
Synthetic biodegradable polymers are obtained from :
  renewable resources e.g., Polylactic acid(PLA)
  non – renewable resources like petroleum e.g., Polyglycolic acid (PGA), Polybutylene succinate (PBS), Polybutylene adipate terephthalate (PBAT)
Microbial polymers e.g.,Poly β-hydroxyalcanoates(PHA)

## Slide 15
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Advantages of biodegradable polymers:
Reduced emission of greenhouse gases and bring a general reduction in plastic waste and waste management
Can be broken down by naturally occurring microorganisms
Easy to use and recycle
Consume less energy during manufacture than the conventional plastic material
Do not release harmful products into the environment on decomposition
They decompose more quickly as compared to non-biodegradable polymers

## Slide 16
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
APPLICATIONS:
Organic waste collection and diversion
Agricultural and horticultural sectors (for example, as mulch-films or plant pots)
Food packaging
Disposable tableware
In medicine for drug delivery and dissolvable sutures

## Slide 17
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Class content:
Adhesives
  Epoxy resin

## Slide 18
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Adhesives
Substances used to bind two or more materials firmly by surface attachment due to penetration of adhesive into material and solidification leading to interfacial locking
Natural adhesives- gum, glue, starch
Synthetic adhesives - PF, UF, epoxides
Adhesives are low molecular weight polymers which are dissolved in solvent. A curing agent is added which causes cross-linking to happen and a thermosetting solid polymer is formed
Preferred for bonding of selected group of materials
  PF - rubber
  UF-Wood
  Epoxy resin – metal, wood, glass, concrete, leather

## Slide 19
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Epoxy resins:
They contain the epoxy group, which is a 3 membered ring of an O atom bonded to carbon atoms
Commercially epoxy resins are known as Araldite or Epon
Synthesis : Epoxy resins can be obtained by the condensation reaction between bisphenol A and epichlorohydrin
Bisphenol A
Source:https://www.oatext.com/bisphenol-a-in-odontology-recent-data.php#gsc.tab=0

## Slide 20
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Epichlorohydrin
Source:https://link.springer.com/chapter/10.1007/978-3-319-59375-3_4

## Slide 21
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Synthesis of epoxy resin:
Excess of epichlorohydrin is used so that the end groups are epoxy groups which are very active
When curing agents are added immediately three – dimensional crosslinked structure is formed
Curing agents are diamines, dicarboxylic acids or acid anhydrides
Source:https://link.springer.com/chapter/10.1007/978-3-662-54959-9_7

## Slide 22
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Properties :
Excellent adhesion
Excellent resistance to water, acid, alkali and other
corrosive chemicals
High mechanical strength
Absorb less moisture
Good insulation properties

## Slide 23
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Applications:
Cured epoxies are frequently used in aerospace and defence
They can used to bind glass, metal, leather, wood, ceramic etc
Coated on floor to give it an antiskid layer
Laminating materials
Crease and shrinkage resistance fabrics

## Slide 24
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Class content: Polymers - PMMA
Poly (Methyl Methacrylate)-PMMA
  Synthesis
  Properties
  Applications
  Advantages
24

## Slide 25
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
PMMA :
PMMA formed by free radical polymerization of monomer methyl methacrylate (MMA).
Polymethyl methacrylate structure- vinyl polymer an ester of methacrylic acid (CH2=C[CH3]CO2H)
PMMA an commercial success polymer known as acrylic, acrylic glass by trade names crylux, Plexiglas, acrylate
25
MMA PMMA

## Slide 26
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
PMMA Synthesis :
Monomer synthesis from acetone to MMA
MMA polymerization to PMMA
26

## Slide 27
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
PMMA Properties :
PMMA is amorphous, white highly transparent, thermoplastic material (moldable at 60-80oC )
Dissolves in organic solvents
Has poor scratch resistance
Inert to acid environmental deterioration
27

## Slide 28
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
PMMA Applications:
Acrylic plastic or PMMA finds its application in a variety of industries due to its properties
  Easy processing and cost-effectiveness
  PMMA is processed by injection, compression moulding, extrusion or casting
The extensive polymethyl methacrylate uses are a result of its advantageous properties and adaptability
28

## Slide 29
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
PMMA Applications:
Glass Substitute: Used in aquariums, aircraft canopies and sign boards, display systems
Construction and Design: Windows, doors, panels, canopies etc., due to its excellent properties such as heat insulation and light transmission.
Automobile Industry: Car windows to windshields, car indicator covers, and panels are also made using plexiglass
Healthcare Industry: known as bone cement- Used by orthopaedic surgeons for joint replacement or treating bone damages. Optical fibres used for endoscopy also consist of PMMA.
29

## Slide 30
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
PMMA Applications :
Cosmetic Usage: PMMA used in various beauty products and injectables. It is used in cosmetic procedures that treat acne, facial lines, wrinkles etc.
Lamps and Lighting: Used in LED lights and lamps- street and traffic lights and lighting devices.
Electronic Devices: Used in the display of various electronic equipment, including tv screens, laptops and smartphones.
Solar Devices: In solar panels is a result of its UV stability and light transmission ability.
Other products where this polymer finds its application include paint, furniture and optical fibres used for telecommunication.
30

## Slide 31
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Advantages of PMMA
PMMA has several advantages over other polymers like polycarbonate (PC) and polystyrene etc. It doesn’t scratch easily or yellow over time. Used as an alternative to other transparent polymers
Some of the advantages of PMMA include:
  Economical, Resistance to weathering
  Various colouring options, High Tensile strength
  Easy to process and handle, Versatility, Biocompatibility
  UV-Stability, Durability, Transmittance and better optical clarity
  Recyclable, Polishability and Non-toxic
31

## Slide 32
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Class content:
Polymer Composites
  Kevlar
    Synthesis
    Properties
    Applications
  Reinforced Kevlar composites

## Slide 33
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Polymer composites
Materials made from two or more constituent materials and their properties are not attainable by any individual component alone are called composites
When one or more of the components are polymers they are called polymer composites
Two components are fibre and matrix
  matrix: polyester, epoxy, phenolic, silicone, melamine, vinyl derivatives
  fibers: glass fiber, boron filaments, carbon/graphite fibers, aramid (aromatic polyamide), aluminum fiber
Polymer composite are produced by suitably bonding a fiber material with a polymer resin matrix and curing the same under pressure and heat
Composites have high strength / unit weight

## Slide 34
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Kevlar
An aramid fibre - Aromatic polyamide
Chemical name is poly-paraphenyleneterepthalamide
Synthesis :
Condensation of 1,4 phenylene diamine and 1,4-benzenedicarbonyl chloride
Source:https://mccord.cm.utexas.edu/chembook/page-nonav.php?chnum=8&sect=6

## Slide 35
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Kevlar is very strong material – about 5 times stronger than steel
High strength is due to:
  Many inter chain hydrogen bonds. The inter-molecular hydrogen bonds formed between the carbonyl groups and NH centers
  Additional strength is derived from aromatic stacking interactions between adjacent strands
Source:https://www.nanowerk.com/nanotechnology-news2/newsid=52521.php
Source:https://www.scielo.br/scielo.php?script=sci_arttext&pid=S1516-14392014000500012

## Slide 36
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Properties :
High tensile strength, high modulus of elasticity
High strength to weight ratio
High chemical inertness
Low co-efficient of thermal expansion
Flame resistance
High impact and cut resistance
Textile processibility

## Slide 37
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Applications :
Well known component of personal armor such as combat helmets,
ballistic face mask and ballistic vest, bullet proof vest
Gloves, sleeves, jackets and other articles
Inner lining in bicycle tires
Light weight boat hulls, aircraft panels, race cars, bridge structure,
Roto blades, tennis, cricket bats, and hockey sticks
Fiber is used in woven rope and in cable
As reinforcement in car tires, in car brakes
In the strings of archery bows
Disadvantages:
Special cutting scissors and drilling machines are required
The fibre is hygroscopic- they absorb moisture

## Slide 38
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
  Reinforced Kevlar composites
Kevlar composite is made by combining Kevlar fibre with epoxy resin
Applications :
monocoque bodies of F1 racing cars, helicopter rotor blades, kayaks, tennis and squash rackets

## Slide 39
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Class content:
Polymer Composites
  Carbon fibre
    Synthesis
    Properties
    Applications
  Carbon Fibre Reinforced Polymer(CFRP)

## Slide 40
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Carbon fibres
Fibers about 5–10 micrometers in diameter and composed mostly of carbon atoms
Several thousand Carbon fibres are twisted together to form a yarn which is used as such or woven into fabric
Source:https://www.racecar-engineering.com/tech-explained/how-are-composites-used-in-motorsport/attachment/composites-in-motorsport-carbon-fibre-vs-human-hair/

## Slide 41
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Synthesis:
Each Carbon filament is produced from a precursor polymer like polyacrylonitrile(PAN), pitch etc.
Synthesis of C fibre from polyacrylonitrile (PAN)
polyacrylonitrile (PAN) is obtained from polymerisation of acrylonitrile
Source:https://slideplayer.com/slide/8375801/

## Slide 42
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Polymerisation
Cyclisation at low temperature
Oxidative treatment at high temperature
Graphitisation at 2000oC in an inert atmosphere
Steps involved in the synthesis of Carbon fibre

## Slide 44
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Source:https://www.researchgate.net/figure/Schematic-representation-of-chemical-structure-of-lignin-cellulose-PAN-and-mesophase_fig4_302483625
Structure:
Consists of sheets of carbon arranged in a regular pattern like graphite
but the sheets interlock
In turbostratic carbon fibre the sheets of carbon fibre are haphazardly
folded or crumpled together

## Slide 45
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Properties :
High strength to weight ratio
Corrosion resistant and chemically stable
Good Tensile Strength
Non Poisonous, Biologically Inert
Low Coefficient of Thermal Expansion

## Slide 46
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Applications :
Aerospace, road and marine transport, sporting
goods
Medical applications in prostheses, surgery and x-ray equipment, implants, tendon/ligament repair
Automobile hoods, novel tooling, casings and bases for electronic equipments, EMI and RF shielding, brushes
Audio equipment, loudspeakers for Hi-fi equipment, pickup arms, robot arms

## Slide 47
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Disadvantages:
Process of producing Carbon fibre is expensive due to
large energy expenditure
Volatile byproducts are formed which include HCN

## Slide 48
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Carbon fibre reinforced polymer(CFRP)
The composite is made by reinforcing carbon fibre with epoxy resin matrix
Properties:
light weight
high strength to weight ratio
low coefficient of thermal expansion
high electrical conductivity

## Slide 49
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Class content:
Conducting polymers
  Introduction
  Types of doping
  Applications

## Slide 50
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Conducting polymers
Polymers are generally insulators because the organic molecules of which they are composed have no free electrons to carry current
An organic polymer with highly delocalized pi-electron system, having electrical conductance of the order of an electrical conductor is called a conducting polymer
Also known as synthetic metals

## Slide 51
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Development :
1977 - Heeger, Macdiarmid & Shirakawa demonstrated conductivity of polyacetylene can be increased 13 times by doping with electron acceptors and donors
Norman et. al - achieved conductance of polyacetylene equal to copper
Doping with less than 10% of chemical species results in dramatic changes in electrical, electronic, magnetic and optical properties of polymers – hence it is a new class of polymers
2000 - Heeger, Macdiarmid & Shirakawa won the Nobel prize for Chemistry

## Slide 52
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Examples of polymers which conduct after doping
Source:https://www.researchgate.net/figure/3Molecular-structure-of-some-typical-conducting-polymers_fig2_304023062

## Slide 53
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Conducting polymers conduct electricity due to delocalization of π electrons
An organic polymer can be converted into conducting polymer if it has :
• linear structure
• extensive conjugation in its polymeric back bone
POLYACETYLENE
POLYPHENYLENE
Source:https://www.researchgate.net/figure/Some-Examples-for-Conducting-Polymers_fig4_269993677

## Slide 54
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
These materials in pure form are not conductors but on doping (Introduction of charged chemical species) conduction increases
Types of Doping
Oxidative doping
Reductive doping
Proton doping

## Slide 55
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Oxidative doping (p-doping)
In this process, pi-backbone of a polymer is partially oxidized using a suitable oxidizing agent
This creates positively charged sites on the polymer backbone which are the current carriers for conduction
The oxidizing agents used are Iodine in CCl4, HBF4 etc.
Source:https://polymerdatabase.com/polymer%20physics/Polymer%20Conductivity2.html

## Slide 56
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Reductive doping (n-doping) :
In this process, pi-backbone of a polymer is partially reduced using a suitable reducing agent
This creates negatively charged sites on the polymer backbone which are the current carriers for conduction
The reducing agent used is sodium naphthalide in THF
Source:https://polymerdatabase.com/polymer%20physics/Polymer%20Conductivity2.html

## Slide 57
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Protonic acid doping :
In this technique, current carrying charged species (+ve and –ve) are created by using a protonic acid as dopant
Doping of polyaniline is a typical example of this type of doping
In polyaniline, current carrying charged species (+ve and –ve) are created by protonation of imine nitrogen

## Slide 58
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Partial oxidation
NH4S2O8
Protonation
HCl (1M)
Source:https://www.indiamart.com/proddetail/polyaniline-pani-semi-flexible-rod-polymer-leucoemeraldine-emeraldine-21303398497.html
Cl-
Cl-

## Slide 59
ENGINEERING CHEMISTRY
Module 7- Functional materials-Polymers
Applications :
As electrode material for commercial rechargeable
batteries, for higher power to weight ratio
As conductive tracks on printed circuit boards
As sensors-humidity sensor, gas sensor, radiation sensor, biosensor
In electrochromic display windows
In information storage devices
As film membranes for gas separations
In light emitting diodes
Important materials in microelectronics applications,
electrocatalysis, fuel cell electrodes, reinforced
composites etc.

## Slide 60
Asha A
Department of Science and Humanities
THANK YOU